VILLAGE OF ALDEN

Detailed Specifications

Specification for:

INSTALLATION OF CONCRETE SIDEWALK- within the Village of Alden

1.	Demolition/ Excavation;

The contractor is responsible for removal and disposal of existing sidewalk or excavation to subgrade. Any existing tree roots shall be removed until below the subgrade level. Contractors are not to stockpile materials or debris on public highways.

The subgrade shall be thoroughly compacted and all soft spots removed and replaced by a suitable, approved fill material.

a)	When a fill exceeding one foot in thickness is required, it shall be thoroughly compacted by tamping

in layers not exceeding six (6) inches.

2.	Base;

The contractor shall supply and install a compacted stone base course for all sidewalks. Base course is to be a minimum of 4” depth of #1 crushed limestone or #1 crusher run limestone per NYS DOT specifications. Base course is to be compacted prior to placing concrete sidewalk.

3.	Concrete;

Redi-Mix concrete shall be 4000 psi Class “D” concrete as per NYSDOT specifications.

4.	 Sidewalk Installation;

a)	Sidewalks shall conform to the specifications hereinafter set forth or as approved by the Village.
	b)	All sidewalks must be set to the grade and line established by the Village.
	c)	THICKNESS — the walk shall not be less than 4 inches thick. Across driveways it shall be

increased to 6 inches thickness.

d)	The walk must have a cross-slope pitch of one-quarter (1/4) inch per foot towards the roadway.

e)	The sidewalk width shall be five (5) foot, or to match adjoining sidewalks.

f)	JOINTS — All walks abutting or adjoining any building, foundation, existing sidewalks, or rigid structure shall have a 3/8-inch expansion joint running the entire length of said walk.

g)	EXPANSION JOINTS — shall be provided at all intersecting walks, drives, curbs and other flat concrete surfaces. Expansion joints shall be provided every 100 feet of run.

h)	JOINTING — The walk shall be cut into separate rectangular slabs not greater than 5 feet on any one side, the surface edges of each slab shall be rounded to a ¼ inch radius and markings shall be exactly at cuts between slabs, unless otherwise specified.

i)	FINISH — Finish shall be fine bristle broom finish.

j)	CURING — All concrete sidewalks must be cured and kept moist for a period of not less than one week. Curing must be accomplished by using an approved curing compound.

- PROTECTION — When completed, the sidewalk must be protected from traffic and elements for at

least one week. In cold weather concrete shall be protected from freezing by blankets or other suitable means. Contractor is responsible for maintaining vehicular access to commercial properties throughout construction.

l)    Reinforcement – all sidewalks through driveways are to be reinforced with 6x6 wire mesh.

- All excavated materials are to be removed from site.

- Existing conditions- contractor is to saw cut all existing driveways and sidewalks at removal points. Contractor is responsible for restoration of all driveways, sidewalks, and grass areas. All areas are to be restored with in-kind materials and quality of installation.

- Contractors are not to wash out concrete trucks or equipment on public roadway or right-of-way (R.O.W.).